## Slide 1: Lotus SPR001
Location of installation: NTPC
Name: Nidhi Dubey
Date 12/03/2024
Time 19:00 hrs.(IST)
Notes: Guru – Testing team

## Slide 2: System Update
Completed Run Hours |  | 939 hrs. | 
Start date | 2023-12-02 16:17:10 | Last updated | 2024-03-12 17:42:10
System Update |  |  |  | 
Date | 12-03-2024 |  | Shift | B
System | Status | Running mins | Shift Engineer | Karthikeyan N
SPR001 | OFF | 270 | Stack | 163-112
Total Running Hours |  |  | 291.5 | 
Running Hours with Dryer |  |  | 10.15 | 
Hours of H2 given to Customer |  |  | 0.00 | 
REMARKS |  |  |  | 
SPR001 |  |  |  | 
1.09:38hrs - System water loop started 2.10:14hrs -Embedded team took control of the system to resolve firmware issues and will be continued tomorrow. 3.13:15hrs- System powered up to 500amps,dryer bypassed. 4.17:44hrs- System powered to zero amps. 5.System is under cold standby mode. |  |  |  | 
Description | Stack L1 |  | Stack L2 | 
Stack Id | 162-112 | Dummy | Dummy | 163-112
Date Start | 02-Nov | 09-Jan | 02-Nov | 09-Jan
Date End | 09-Jan | Prst. | 09-Jan | Prst.
Note | The data points in all the LHC & LWC Charts are depicted as average of per hour data (not in Voltage related charts & last 24 hrs charts). |  |  | 
Summary | System working with stack 163-112 at L2 & L1-Dummy (These are electrical connections). Latest steady state Current Density is ~0.42 A/cm2. Max Voltage at 0.92 A/cm2 was 1.633 V. |  |  | 

## Slide 5: LHC Charts – cv and cd (last 24 hrs.)

## Slide 6: LHC Charts – cv and cd

## Slide 7: LWC Charts
PMP State: 1 : ON 0 : OFF

## Slide 8: LWC Charts - last 24 hrs.
PMP State: 1 : ON 0 : OFF

## Slide 9: Thank you!