## Slide 1: Lotus Unit 0002
Location of installation: CKB Test Bed
Name: Nidhi Dubey
Notes: Guru – Testing team

## Slide 2
System Id | SPR001 | Location | ntpc | Completed Run Hours |  |  | 
 |  |  |  | Start date |  | Last updated | 
Description | U1 |  |  |  | U2 |  |  |  | L2 |  |  |  | L1 |  |  | 
Stack Id |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Date Start |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Date End |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Note | The data points in all the LHC Charts except the pol curves are depicted as average of per hour data. |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Summary |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 4: LHC Charts – CV and Id (24 hours)

## Slide 5
LHC Charts – ASR

## Slide 6: LHC Charts – Polarization Curves

## Slide 7: LHC Charts – Stack-wise Polarization Curves

## Slide 8: LWC Charts – Last 24 hrs.
PMP State: 1 : ON 0 : OFF

## Slide 9: System Update
Completed Run Hours |  | 506 hrs. | 
Start date | 2023-12-02 16:17:10 | Last updated | 2024-01-16 15:23:50
System Update |  |  |  | 
Date | 16-01-2024 |  | Shift | B
System | Status | Running mins | Shift Engineer | Stefy
SPR001 | OFF | NIL | Stack | 163-112
Total Running Hours |  |  | 213.85 | 
REMARKS |  |  |  | 
SPR001 |  |  |  | 
07:45 System Water loop started. 09:15 System started and current increased till 650A. HYS102 checked. Dryer Bypassed. 10:49 Power Outage in Customer side. 10:56 System started and current increased till 650A.Dryer Bypassed. 12:35 Power Outage in Customer side. 12:43 System started and gradually current increased till 650A 14:15 System stopped and in Hot Standby Mode 20:20 System was in hot standby mode till 20:20hrs. 20:21hrs - System in cold standby mode. |  |  |  | 
Description | Stack L1 |  | Stack L2 | 
Stack Id | 162-112 | Dummy | Dummy | 163-112
Date Start | 02-Nov | 09-Jan | 02-Nov | 09-Jan
Date End | 09-Jan | Prst. | 09-Jan | Prst.
Note | The data points in all the LHC & LWC Charts are depicted as average of per hour data (not in Voltage related charts & last 24 hrs charts). |  |  | 
Summary | System working with stack 163-112 at L2 & L1-Dummy (These are electrical connections). Latest steady state Current Density is ~0.92 A/cm2. Max Voltage at 0.92 A/cm2 was 1.753V. |  |  | 

## Slide 10: System Update
Completed Run Hours |  | 647 hrs. | 
Start date | 2023-12-02 16:17:10 | Last updated | 2024-01-31 20:03:15
System Update |  |  |  | 
Date | 31-01-2024 |  | Shift | B
System | Status | Running mins | Shift Engineer | Stefy
SPR001 | Water loop | 122 | Stack | 163-112
Total Running Hours |  |  | 236.45 | 
REMARKS |  |  |  | 
SPR001 |  |  |  | 
1. 9:11hrs - water loop started, TTC-102 - 16.4 deg. C, amb temp at site - 12 deg. C. 2.10:48hrs - system stopped. 3.11:12hrs - System restarted - hot standby mode. 4. 11:58hrs - System powered up - 20A given. 5. 12:12hrs - System in hot standby mode. 6. 12:26hrs - System powered up -20 A given - to check fluctuations in VSC. 7. 13:30hrs - System in hot standby mode. 8. 14:00hrs - System in hot standby mode. 9. 14:35 System powered up with 20A. (site visit) 10. 14:37- system current =50A. 11. 14:40- System current reduced to 20A to verify HYS-102. 12. 14:48- Current=100A, TTC-102= 27.6, COS-101=0.8. 13. 14:50- Current= 200A, TTC-102= 28.3, COS-101=0.7 14. 14:55- Current= 300A, TTC-102= 29.3, COS-101=0.5 15. 16:34 - Current reduced to 20A 16. 6:38- Current reduced to 0A.- water loop in progress- System in Hot standby. 17. 20:00- System in cold standby. (Heavy Rain at site) Received 2 new N2 cylinders and verified it's 170bar. |  |  |  | 
Description | Stack L1 |  | Stack L2 | 
Stack Id | 162-112 | Dummy | Dummy | 163-112
Date Start | 02-Nov | 09-Jan | 02-Nov | 09-Jan
Date End | 09-Jan | Prst. | 09-Jan | Prst.
Note | The data points in all the LHC & LWC Charts are depicted as average of per hour data (not in Voltage related charts & last 24 hrs charts). |  |  | 
Summary | System working with stack 163-112 at L2 & L1-Dummy (These are electrical connections). Latest steady state Current Density is ~0.42 A/cm2. Max Voltage at 0.42 A/cm2 was 1.728V. |  |  | 

## Slide 11: Thank you!