## Slide 1: Lotus Unit 0008
Location of installation: CKB Test Bed
Name: Nidhi Dubey
Notes: Guru – Testing team

## Slide 2
System Id | U0008 | Location | CKB | Completed Run Hours |  |  | 
 |  |  |  | Start date |  | Last updated | 
Description | U1 |  |  |  | U2 |  |  |  | L2 |  |  |  | L1 |  |  | 
Stack Id |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Date Start |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Date End |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Note | The data points in all the LHC Charts except the pol curves are depicted as average of per hour data. |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Summary |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 3: LHC Charts
Latest steady state Current Density is ~0.71 A/cm2.
Stack Temperature is ~50-60 deg C.
COS 101 varies between 0-1.4 µS/cm on 10 Oct.

## Slide 4: LHC Charts – Cell Voltage
System lately working with stacks installed at all four positions.
Latest steady state Current Density was ~0.71 A/cm2.
Max Cell Voltage at 0.26 A/cm2 is 1.887 V.

## Slide 5: LHC Charts – ASR
In the last steady state cd, the ASR was ~2800 mΩ-cm2.

## Slide 6: LHC Charts – Polarization Curves
1. Pol curve is plotted for the average Cell V
vs. Current density.
2. The whiskers in the pol curves are the
min and max values.

## Slide 7: LHC Charts – Stack-wise Polarization Curves

## Slide 8
LWC Charts
PMP State: 1 : ON 0 : OFF
Lately LWC conductivity COS 701 varies between 0-5 µS/cm and COS702 varies between 5.5-6.5 µS/cm.
PRT 704 was bar & PRT 705 varied between - bar on 13th oct.

## Slide 9: Thank you!